# EMIRATES AUTHORITY For  STANDARDIZATION & METROLOGY

(ESMA)

# FINAL DRAFT

# UAE STANDARD

# LUBRICATING OILS FOR INTERNAL

# COMBUSTION ENGINES

------------------------------------------------------------------------------------------------

THIS DOCUMENT IS A DRAFT STANDARD CIRCULATED FOR COMMENTS.  IT IS, THEREFORE, SUBJECT TO CHANGE AND MAY NOT BE REFERRED TO AS A UAE STANDARD UNTIL APPROVED BY THE BOARD OF ESMA

# LUBRICATING OILS FOR INTERNAL

COMBUSTION ENGINES

1	SCOPE AND FIELD OF APPLICATION

This standard is concerned with lubricating oils for internal combustion engines suitable for gasoline and diesel engines service excluding marine application.

2	COMPLEMENTARY REFERENCES" .*

2.1	GS 126/1990 " Method of Sampling Oils .

2.2     GS 130/1990 "Methods of Testing for Lubricating oils: Determination of Sulfated Ash for Lubricating Oils and Additives” .

2.3	GS  873/1997 " Determination of Apparent Viscosity for Engine Oils at Low Temperature Using the Cold Crank Simulator".

2.4	GS 896/1997 " Determination of Phosphorous Content in Lubricating Oils  and Additives".

2.5   GS 1068/2003 " Determination of Kinematics Viscosity and Dynamic Viscosity For Petroleum Products ".

3	DEFINITIONS

3.1	Mineral oil: Petroleum product produced after refining (separating fuel distillates) by extracting asphalt, aromatics, resins, unstable materials, wax and moisture to improve its characteristics.

3. 2	Base stock: Mineral or synthetic oil or mixture of both.

3. 3	Additives: Chemical materials designed to be mixed with base stocks to enhance its performance properties.

3. 4	Lubrication: The act of adding lubricating oil to reduce friction and wear between the moving parts, to control the increase in temperature rise caused by the friction, to minimize corrosion and to remove residues resulting from internal combustion.

* Note: All the international and other  standards that referred to them in the tables (appendix of this standard) are regarded as complementary references including test methods for determination of conradson carbon residue ASTM D189 and sulfur content ASTM D2622 or equivalents   .

4	CLASSIFICATION

Lubricating oils are classified according to their viscosity and performance as follows:

4. 1	Classification according to viscosity

Lubricating oils are classified according to viscosity based on SAE classification J 300/ 2004 [see Table(1) in (Appendix)].

Multigrade oils are the combination of winter (W) and summer grades.

4. 2	Classification according to performance for Gasoline Engine oils

Table (2) based on API Classification (service category “S”).

The lubricants covered by these categories are for gasoline passenger cars, some trucks and off-highway equipment.

NOTE: The letter  following service category “S”  indicates the    performance category of the oil.

# 4. 2.1    SJ-1997 Gasoline Engine Service

Category SJ was adopted in 1996 to describe engine oil first mandated in 1997. It is for use in service typical of gasoline engines in present and earlier passenger cars, vans and light trucks operating under vehicle manufacturers’ recommended maintenance procedures. Oils meeting API SJ requirement have been tested according to the American Chemistry Council (ACC) Product Approval Code of Practice and may utilize the API Base Oil Interchange and Viscosity Grade Engine Testing Guidelines. They may be used where API Service Category SH and earlier categories are recommended.

NOTE: SJ represents the minimum category used in this Gulf standard and can be used where the earlier obsolete service categories SA, SB, SC, SD, SE, SF, SG and SH are recommended.

# 4. 2. 2     SL-2001 Gasoline Engine Service

Catorgy SL was adopted to describe engine oils for use in 2001.These oils are  use in service typical of gasoline engines in present and earlier passenger  cars , sport utility vehicles, vans and light trucks operating under vehicle manufacturers’ recommended maintenance procedures.  Engine oils that meet API service category SL designations have been tested according to the American Chemistry Council (ACC) Product Approval Code of Practice and may utilize the API Base Oil Interchange and Viscosity Grade Engine Testing Guidelines. They may be used where API Service Category SJ and earlier categories are recommended.

# 4. 2.3      	SM-2005 Gasoline Engine Service

Category SM was adopted for use in describing engine oils available in 2004 .These oils are for use in service of gasoline engines in current and earlier passenger cars, sport utility vehicles, vans, and light-duty trucks operating under vehicle manufacturers recommended maintenance procedures.

Engine oils that the API Service Category SM designation may be used where API Service Category SL and earlier S Categories have been recommended.

Engine oils meeting API Service Category SM requirements have been tested according to “American Chemistry Council (ACC) Product Approval Code of Practice” and may utilize the API Base Oil Interchangeability and Viscosity Grade  Engine Testing Guidelines.

  - Classification according to performance for Diesel Engine Oils

Tables (3) based on API classification (service category “C”).

The lubricants covered by this category cover diesel engine trucks and      diesel powered off-highway equipment (fleets, contractors, farmers, etc.).

NOTE: The letter following service category “C” indicates the performance category of the oil.

# 4.3.1         CF - For off- road Indirect Injected Diesel Engine Service

Service typical of off-road,  indirect injected diesel engines and other diesel engines that use a broad range of fuel types including those using fuel with higher sulfur content, for example; over 0.5% wt. Effective control of piston deposits, wear, and corrosion of copper-containing bearing is essential for these engines, which may be naturally aspirated, turbocharged, or supercharged.  Oils designated for this service have been in existence since 1994.  Oils designated for this service may also be used when Service Category CD is recommended.

NOTE: CF represents the minimum category used in this standard and       covers the earlier obsolete categories CA, CB, CC, and CD.

# 4. 3.2	CF-2 Severe Duty Two-Stroke Cycle Diesel Engine Service

Service Category CF-2 denotes service typical of two-stroke cycle engines requiring highly effective control over cylinder and ring-face scuffing and deposits.  Oils designated for this service have been in existence since 1994 and may also be used when API Service Category CD-II is recommended.  These oils do not necessarily meet the  requirements of CF or CF-4 unless passing test performance requirements for these categories.

# CF-4-1990 Diesel Engine Service

Service Category typical of CF-4 describes oils use in high speed, four- stroke cycle diesel engine.  CF-4 oils exceed the requirements of Service Category CE, are designed to replace CE oils and provide improved control of oil consumption and piston deposits.  CF-4 oils may be used in place of CC and CD. They are particularly suited for on-highway heavy duty truck applications.

# 4. 3.4	CG-4 -1994 Severe Duty Diesel Engine Service

Service Category CG-4 describes oils for use in high speed four stroke-cycle diesel engines used on highway and off highway applications where fuel sulfur may vary from less than 0.05 percent by weight to less than 0.5 percent by weight.  CG-4 oils provide effective control over high temperature piston deposits, wear, corrosion, foaming, oxidation stability and soot accumulation.  These oils are especially effective in engines designed to meet 1994 exhaust emission standards and may also be used in engines requiring service categories CD, CE and CF-4.  Oils designated for this service have been in existence since 1995.

# 4. 3. 5    CH-4- 1998 Severe – Duty Diesel Engine Service

API Service Category CH-4 describes oils for use in high speed, four- stroke cycle diesel engines used in highway and off-road applications. CH-4 oils provide effective control over engine deposits, wear, corrosion, oxidation stability and soot accumulation. These oils are especially effective in engines designed to meet 1999 emission standard and may also be used in engines requiring API Service Category CG-4. Oils designated for this service have been in existence since 1999.

CH-4 oils are engineered for use with diesel fuels ranging in sulfur content up to 0.5% weight .

# 4. 3. 6  CI-4-2002 Severe Duty Diesel Engine Service

# The API CI-4  Service category describes oils for use in those high – speed , four- stroke cycle diesel engines designed to meet 2004 exhaust emission standards and was implemented in October 2002 . These oils are compounded for use in all applications with diesel fuels ranging in sulfur content up 0.05% by weight . These oils are especially effective

at sustaining engine durability where Exhaust Gas Recirculation (EGR) and  other exhaust emission componentry may be used . Optimum protection is provided for control of corrosive wear tendencies , low and high temperature stability , soot handling properties, piston deposit control , valvetrain wear , oxidative thickening , foaming and viscosity loss due to shear . API CI-4  oils are superior in performance to those meeting API CH-4, CG-4  and CF-4  and can effectively lubricate engines calling for those API Service Categories.

4. 3. 7  CI-4 PLUS in Conjunction with API Service Category CI-4

API Service  Category CI-4 engine oils that also carry the classification CI-4PLUS are formulated to provide a higher level of protection against soot-related viscosity increase and viscosity loss due to shear in vehicles powered by diesel engines. Oils that satisfy CI-4, CH-4,CG-4 and CF-4 and can effectively lubricate engines calling for those API Service Categories.

5	CHARACTERISTICS

The lubricating oils shall fulfill the following characteristics:

5. 1	They shall be homogeneously mixed, bright and clear and have acceptable odour.

5. 2	They shall be free from water, sediments, dusts, abrasive matter and impurities

5. 3	They shall contain some additives as; anti-oxidation, anti-rust, anti-corrosion, anti-wear, anti-foam, detergents/dispersants and pour point depressant and others, etc. to improve the quality and meet performance requirements of Tables 2 and Tables 3 (see Appendix ).

5. 4	The additives (item 5.3), to be used shall be completely soluble in the base oil. They shall neither partly precipitate nor separate if the temperature raised to 125oC.

5. 5	The base oils to be used with the additives (item 5.4) shall be paraffinic base oils with viscosity index V.I≥90 and conforms to API classification of base oils given in Table 5 (see Appendix ).

No re-refined or recycled Base Oils to be used in formulating these lubricants unless these oils are produced by internationally recognized licensed processes and the base oil products have the same quality of virgin Base Oils and conform  to the API classification of Bas oil given in Table 5 (see Appendix)

5. 6     They shall fulfill the pour point and flash point requirements of Table 4 (see Appendix ).

5. 7	The viscosity index of the oils shall not be less than 90.

5. 8	The value of phosphorus, zinc, and other metals, sulphated ash, total acid number, total base number, and shall be mentioned as guidelines and reported in the test report.

5. 9	The oils shall be stable and compatible.

6	SAMPLING

Samples shall be drawn according to Standard mentioned in item (2.1).

7	METHODS OF TESTING*

The following tests shall be carried out according to the performance and application requirement and the representative sample taken in accordance with item (6).

# 7. 1	Physical & Chemical Tests

# 7.1.1	Visual inspection.

7.1.2	Determination of flash and fire points.

# 7.1.3	Determination of kinematics viscosity and dynamic viscosity.

7.1.4	Calculation of viscosity index.

# 7.1.5	Determination of pour point.

7.1.6	Determination of phosphorus content.

# 7.1.7	Determination of zinc content.

# 7.1.8	Determination of calcium content.

# 7.1.9	Determination of magnesium content.

# 7.1.10	Determination of sulphated ash.

# 7.1.11	Determination of nitrogen content.

# 7.1.12	Determination of total base number.

# 7.1.13	Determination of foaming characteristics of lubricating oils.

# 7.1.14   Determination of stability and compatibility.

# 7.1.15   Determination of homogenously solubility.

# 7.1.16   Determination of apparent viscosity.

# 7.1.17   Determination of pumping viscosity.

# 7.2	Engine and Bench Tests

# For the evaluation of lubricating oils used in internal combustion engines, as listed in Tables 2 and 3 (see Appendix).

*Note	1) The tests shall be carried out according to the Standards given in item (2) or equivalents and according to international test methods standards  ( ISO or ASTM or IP)

2) Engine Test Requirements and Testing Methods for Gasoline and         Diesel Engines Oils shall be carried out according to ASTM Standards mentioned  in the Table 6 and Table 7  (see Appendix).

8	PACKING

Lubricating oils shall be packed in tightly closed and sealed  containers preventing possibilities of oil leakage or oil contamination with any impurities;

such containers neither shall affect nor be affected by the oil.

9	LABELLING

The following information shall be legibly and indelibly marked in both Arabic and English languages on each container of lubricating oils.

9.1       Net volume, in liters.

# 9.2       Producer’s name or his registered trade mark.

9.3       Name of the country of origin.

# 9.4  The classification of oils according to SAE viscosity, and API   performance (as in item 4).

9.5        Date of production and the batch number

9.6   Precaution : “Avoid Environmental Pollution" or use “International symbol for no pollution"

9.7        Base Oil origin virgin base oil or recycled.

10	RULES FOR ACCEPTANCE AND REJECTION

10.1	Each consignment of lubricating oils shall be accompanied with a certificate stating its compliance with this standard.

10.2	The consignment shall be considered complying with this Gulf standard when the accompanying certificate is accepted.

10.3	In case the certificate is not accepted (because information is incomplete or subject to question), the information may be completed or (if necessary) substantial test mentioned in item (7.1) shall be carried out on samples taken in accordance with all the requirements of this standard.  When the withdrawn samples pass all the test the consignment shall be considered as complying with this standard.  In case one or more of the lubricating oil samples fail to pass any of the tests, a second sample, double the number of samples of the first one shall be withdrawn from the same group and subjected to all the tests.

The consignment shall be considered as complying with the requirements of this standard when all the test samples of the second sample pass the re-tests.  Otherwise the consignment shall be considered as not complying.

APPENDIX

# TABLES

| TABLE (1) | : | SAE Viscosity Grades for Engine Oils |
| --- | --- | --- |
| TABLES (2) | : | Performance Characteristics of Lubricating Oil for Gasoline Engine |
| TABLES (3) | : | Performance Characteristics of Lubricating Oil for Diesel Engine |
| TABLE (4) | : | Pour Point and Flash Point of Engine Oils |
| TABLE (5) TABLE (6) TABLE (7) | : : : | API Classifications of Base Oil Groups Gasoline Engine oils Classification , Engine Test Requirements and ASTM Methods Diesel Engine oils Classification , Engine Test Requirements and ASTM Methods |

Table(1)

SAE VISCOSITY GRADES FOR ENGINE OILS J 300/04

| SAE Viscosity grade | Low –temperature (oC) Cranking Viscosity (3), mPa.s max. | Low temperature (oC) Pumping Viscosity (4), cp max. with no yield stress | Low-Shear-Rate Kinematic Viscosity (5) (mm2/s) at 100 oC min. | Low-Shear-Rate Kinematic Viscosity (5) (mm2/s) at 100 oC max. | High-shear-Rate Viscosity (6) cP at 150 oC and 106 S-1 min. |
| --- | --- | --- | --- | --- | --- |
| 0 W | 6200 at -35 | 60 000 at -40 | 3.8 | - | - |
| 5 W | 6600 at -30 | 60 000 at -35 | 3.8 | - | - |
| 10 W | 7000 at -25 | 60 000 at -30 | 4.1 | - | - |
| 15 W | 7000 at -20 | 60 000 at -25 | 5.6 | - | - |
| 20 W | 9500 at -15 | 60 000 at -20 | 5.6 | - | - |
| 25 W | 13000 at -10 | 60 000 at -15 | 9.3 | - | - |
| 20 | - | - | 5.6 | < 9.3 | 2.6 |
| 30 | - | - | 9.3 | < 12.5 | 2.9 |
| 40 | - | - | 12.5 | < 16.3 | 2.9 (0W-40, 5W-40 and 10W-40 grades) |
| 40 | - | - | 12.5 | < 16.3 | 3.7(15W-40,20W-40, 25W-40,40 grades) |
| 50 | - | - | 16.3 | < 21.9 | 3.7 |
| 60 | - | - | 21.9 | < 26.1 | 3.7 |

# (1)    Notes   1 mPa.s=1 cP;  1 mm2/s = 1 cSt

(2)    All values are critical specification as defined by ASTM D3244

(3)    ASTM D5293.

(4)    ASTM D4684 :    Note   that the presence of any yield stress detectable by this method constitutes a failure regardless of viscosity.

(5)    ASTM D445.

(6)    ASTM D4683, CEC L-36-A-90 (ASTM D4741), or ASTM D5481.

Table(2-0)

# API " S.." (GASOLINE) SERVICE CATEGORIES

ENGINE AND BENCH TEST REQUIREMENT SUMMARY

| (SM) | (SL) | SJ)) | (SH) | (SG) | (SF) | (SE) | API CATERGORY | ( SD) | (SC) | (SB) | (SA) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Grade |
| Current | Current | Current | Obsol. | Obsol. | Obsol. | Obsol. | Timing | Obsol. | Obsol. | Obsol. | Obsol. |
| - X X - IIIG IVA VG - - | - X X - IIIF IVA VG - - | X or VIII - - IID or BRT IIIE or IIIF - VE or VG+IVA - - | X - - IID IIIE - VE - - | X - - IID IIIE - VE 1 H2 - | X - - IID IIID - VD - - | X - - IID IIIC or IIID - VC or VD - - | 38 L - Ball Rust Test SEQ. VIII SEQ. II SEQ. III SEQ. IV SEQ. V CATERPILLAR FORD FALCON | X - - IIB IIIB IV VB L 1 or 1 H X | X - - IIA IIIA IV V - - | X - - - - IV - - - | None |
| SAE J 300 X X X - X MHT-4 X X | SAE J 300 X X X - X MHT-4 X - | SAE J 300 X X X X X D6335 X X | SAE J 300 X X X X X X - X | SAE J 300 - - - - - - - - | SAE J 300 - - - - - - - - | SAE J 300 - - - - - - - - | Viscometrics Volatility Filterability Foaming Flash point Homog. & Miscibility TEOST Gelation index L-38 Shear Stability | SAE J 300 - - - - - - - - | SAE J 300 - - - - - - - - | SAE J 300 - - - - - - - - | SAE J 300 - - - - - - - - |

# Table (2-1)

# API " SJ " (GASOLINE) SERVICE CATEGORIES

| API SJ |
| --- |
| others | 10W-30 | 5W-30 | 5W-20 | 0W-20 | SAE Viscosity grades |
| 15(7) 20(7) 50 to report 10 / 03 50 / 03 10 / 03 200/504 - - pass to report SAE J300 SAE J300 SAE J300 SAE J300 SAE J300 SAE J300 SAE J300 SAE J300 60 - | 17 22 50 to report 10 / 03 50 / 03 10 / 03 200/504 200 185 pass 0.10 9.3 12.5 2.9 - <7000 >6600 - -30 60 12 | 17 22 50 to report 10 / 03 50 / 03 10 / 03 200/504 200 185 pass 0.10 9.3 12.5 2.9 - - <6600 >6200 -35 60 12 | 17 22 50 to report 10 / 03 50 / 03 10 / 03 200/504 200 185 pass 0.10 5.6 9.3 2.6 - - <6600 >6200 -35 60 12 | 17 22 50 to report 10 / 03 50 / 03 10 / 03 200/504 200 185 pass 0.10 5.6 9.3 2.6 - - - <6200 -40 60 12 | Bench Test Requirements ASTM D6417 or ASTM D5480(1), simul.distill. % max. ASTM D5800(1), evapor. Loss, % max Filterability(2), % flow reduction, max, EOFT , standard Procedure EOWTT, Modif, Proced. With 0.6, 1.0, 2.0, 3.0 % H2O Foaming ASTM D892 option A, Sequence I, max. Sequence II, max. Sequence III, max. High temp. foaming, ASTM D6082, static foam, max. ASTM D92(5), flash point, oC, min. ASTM D93(5), flash point, oC, min. FTM 791C method 3470, (Homog. & Misc.) ASTM D4951 or D5185 Phosphorus, wt %, max.(6) ASTM D445, Kinem. Viscosity at 100 oC, cSt, min. max. ASTM D4683, HT/HS viscosity, mPa.s, min. SAE J300, apparent viscosity, cP at -15 o C at -20 o C at -25 o C at -30 o C ASTM D4684, pumpability, 60.000cP max. At o C ASTM D6335 high temp.deposits (TEOST), mg, max. ASTM D5133, gelation index, max. |

BENCH TEST LIMITS

(1) Meet the volatility in either ASTM D6417, or ASTM D5800 or ASTM D5480.             (2) Formerly known as GM 9099P.                                                   (3) 10 seconds settling.

# (4) 1minute settling.                                                                                                                 (5) Either D92 or D93  may be used.                                                 (6)  Non critical spec. per ASTM D3244.

(7) SAE 15W-40 only tu

# Table (2-2)

# API "SL" (GASOLINE) SERVICE CATEGORIES

BENCH TEST LIMITS

| API SL |
| --- |
| All others | 0W-20, 0W-30, 5W-20, 5W-30, 10W-30 | SAE Viscosity grades (a) |
| 15 10 50 50 10 / 0(1) 50 / 0(1) 10 / 0(1) 100 / 0(1) pass Not Required SAE J300 SAE J300 SAE J300 SAE J300 45 Not Required | 15(4) 10(4) 50 50 10 / 0(1) 50 / 0(1) 10 / 0(1) 100 / 0(1) pass 0.10(2) (5) SAE J300 SAE J300 SAE J300 SAE J300 45 12(5) | Bench Test Requirements ASTM D5800(4), evaporation loss, % max. ASTM D6417(4), simulated distillation, % max Filterability, % flow reduction, max, EOFT , standard Procedure EOWTT, modif, Proced. With 0.6, 1.0, 2.0, 3.0 % H2O Foaming ASTM D892 option A, Sequence I, max. Sequence II, max. Sequence III, max. High temp.foaming, ASTM D6082, static foam max. FTM 791C method 3470, (H & M) ASTM D4951 or D5185 Phosphorus, wt %, max.(5) ASTM D445, Low-Shear-rate kinematic viscosity@100oC ASTM D4683, High-Shear-rate kinematic viscosity@150oC. ASTM D5293, Low temperature cranking viscosity ASTM D4684, Low temperature pumping vis.,no yield stress TEOST MHT4, high temperature deposits, mg deposit, max. ASTM D5133.gelation index, max.(5) |

(a) All oils meet the requirements of the most recent edition of SAE J300

(1) 10 minutes settling for Seq. I, II, III.                                                      (2) Non critical spec. as described in ASTM D3244.                                                                                       (3) 1 minute settling.

(4) Must run both D5800 and D6417.                                                        (5) Requirement applies only SAE 0W-20, 5W-20, 0W-30,5W-30 and 10W-30 viscosity grades.

# Table (2- 3)

# API " SM" (GASOLINE) SERVICE CATEGORIES

# BENCH TEST LIMITS

| API SM |
| --- |
| All Others | 0W-20, 5W-20, 0W-30, 5W-30, 10W-30 | SAE Viscosity grades requirements |
| 100 15 10 50 50 50 50 50 NR 0.06d NR NR 10/0 50/0 10/0 100/0 g h 45 NR | 100 15 10 50 50 50 50 50 0.08d 0.06d 0.5d 0.7d 10/0 50/0 10/0 100/0 g h 35 12i | Bench Test Requirements ASTM D6557 (Ball Rust Test), avg. gray value, min. ASTM D5800, evaporation loss, 1 hour at 250oC,% maxb ASTM D6417 simulated distillation at 371oC, % max ASTM D6795, EOFT,% flow reduction, max ASTM D6795, EOWTT, % flow reduction, max With 0.6%H2O With 1.0%H2O With 2.0%H2O With 3.0%H2O ASTM D4951, phosphorus % mass max.c ASTM D4951, phosphorus % mass min.c ASTM D4951 or D2622, sulfur% mass, max.c SAE 0W-20, 0W-30,5W-20, and 5W-30 SAE 10W-30 ASTM D892 (optional A), foaming tendency Sequence I, ml, max, tendency/stability Sequence II, ml, max, tendency/stability Sequence III, ml, max, tendency/stability ASTM D6082 (option A), high-temperature foaming Ml, max, tendency/stability ASTM D6922, homogeneity and miscibility ASTM D6709, (Sequence VIII) shear stability TEOST MHT, high temperature deposits, deposit wt,mg, max. ASTM D5133, gelation index, max. |

# Note: All Oils must meet the requirements of the most recent edition of SAE J300; NR=Not Required

aTests are per ASTM requirements.

b Calculated conversions specified in ASTM D 5800 are allowed.

cFor all viscosity grades: If CF-4,CG-4,CH-4 and/or Cl-4 categories precede the ‘S’ Category and there is no API certification

Mark, the limits  for phosphorus, Sulfur, and the TEOST MHT do not apply. Note that these oils have been formulated

primarily for diesel engines and may not  provide all of the performance requirements consistent with vehicle manufacturers recommendations for gasoline-fueled engines

dThis is a non-critical specification as described in ASTM D3244.

eAfter 10-minute settling period.

fAfter 1-  minute settling period.

gShall remain homogenous and, when mixed with ASTM reference oils, shall remain miscible.

hTen-hour stripped kinematic viscosity at 100oC. kinematic viscosity must remain in original viscosity grade.

jTo be evaluated from -5oC to temperature at which 40.000 cP is attained or -40oC, or 2 Celsius degree below the appropriate MRV TP-1  temperature (defined by SAE J300), whichever occurs first.

# Table (2- 4)

# API " S.." (GASOLINE) SERVICE CATEGORIES

ENGINE TEST LIMITS-1

| API | Letter designation | API |
| --- | --- | --- |
| (SM) | (SL) | (SJ)(4) |  | (SH) | (SG) | (SF) |
| all | all | all | SAE Viscosity grades | all | all | all |
| - - - | - - - | 40 - stay in grade | CRC L- 38 Bearing weight loss, mg max. Piston skirt varnish, min. 10h. stripped viscosity | 40 - stay in grade | 40 9.0 stay in grade | 40 - - |
| 26 max - | 26.4 stay in grade | - - | SEQUENCE VIII Bearing weight loss, mg, max 10h. stripped viscosity | - - | - - | - - |
| - - - - | - - - - | 8.5 - - none | SEQUENCE IID Average engine rust, min. Avg. crankcase pressure, in. H2O, max. Max. crankcase pressure, in. H2O, max. Lifter sticking, max. | 8.5 1.3 3.0 none | 8.5 - - none | 8.5 - - none |
| 100 | 100 | - | Ball Rust Test (BRT) Average gray value, min. | - | - | - |
| IIIG 150%Max. - - Drop - 3.5 min. none - - 60 - 4.65 liter for validity | IIIF 275 - - 9.0 - 4.0 none - - - 20 (2) to report (3) | IIIE - 64 9.2 8.9 3.5 - none(1) none none 64 (0.0025) 30 (0.0012) 5.1 - | SEQUENCE III Viscosity increase at 40oC, %max. at 64h Hours to 375 % vis. inc. at 40oC, min. Average engine sludge, min. Average piston skirt varnish, min. Average oil ring land deposits, min. Weighted piston deposits, min. Ring sticking (hot stuck) Lifter sticking Cam or lifter scuffing Maximum cam + lifter wear, µm (in.), max. Average cam + lifter wear, µm (in.), max. Oil consumption, liter, max. Low temperature viscosity | IIIE - 64 9.2 8.9 3.5 - none(1) none none 64 (0.0025) 30 (0.0012) - - | IIIE - 64 9.2 8.9 3.5 - none(1) none none 64 (0.0025) 30 (0.0012) - - | IIID 375 - 9.2 9.2 4.8 - none(1) none none 203 (0.0080) 102 (0.0040) - - |

(1) An oil related stuck ring occurs on a piston with individual oil ring land deposit rating < 2.6.

(2) Oil consumption is no longer a pass/fail limit. If the oil cons. is >5. 2 .1 for and oil with Noack  volatility <  15% or > 6.5 1. for and oil with Noack volatility >  15%, the test is declared invalid.

(3) Evaluate the 80-hour test oil sample by Test Method D4684 (MRV TP-1) at the temperature indicated by the low temperature grade of oil determined on the 80-hr sample by test method D5293 (CCS Viscosity).            (4) Alternative engine tests may be run instead of those presented as described in ASTM letter of  April 28, 2000.Ball Rust Test instead of Seq. IID, Seq.IVA plus Seq. VG instead of Seq.VE; Seq.VIII instead of L-38, Seq.IIIF as an alternative to the Seq.IIIE but for  this engine  test no official document has been released .Current ASTM D4485-01c does not contain these information yet

# Table (2-5)

API " S.." (GASOLINE) SERVICE CATEGORIES

# ENGINE TEST LIMITS-2

| API | Letter designation | API |
| --- | --- | --- |
| (SM) | (SL) | (SJ)(3) |  | (SH) | (SG) | (SF) |
| all | all | all | SAE Viscosity Grades | all | all | all |
| 90 No IVA required if C category comes first | 120 | - | SEQUENCE IVA cam wear avg, µm, max. | - | - | - |
| VG 7.8 8.0 7.5 8.9 to report 20 to report none to report - - | VG 7.8 8.0 7.5 8.9 to report 20 to report none to report - - | VE(2) - - - - - - - - - 380 (0.015) 127(0.005) | VE 9.0 7.0 6.5 5.0 - 20 to report none - 380 (0.015) 127(0.005) | SEQUENCE V Average engine sludge, min. Rocker arm cover sludge, min. Average piston skirt varnish, min. Average engine varnish, min. Oil screen debris, % max. Oil ring clogging, % max. Oil ring clogging, % max.(1) Compression ring sticking (hot stuck) Cold stuck rings Maximum cams wear, µm (in), max. Average cam wear, µm (in), max. | VE 9.0 7.0 6.5 5.0 - 20 to report none - 380 (0.015) 217 (0.005) | VE 9.0 7.0 6.5 5.0 - 20 15 none - 380 (0.015) 130 (0.005) | VD 9.4 - 6.7 6.6 - 7.5 10.0 none - 64 (0.0025) 30 (0.0012) |

(1) Oil ring clogging as a pass criterion, suspended indefinitely by ASTM on june 1st 94.

(2) Not required for oils containing a minimum of 0.08% mass phosphorus in the form of ZnDTP.

(3) Alternative engine tests may be run instead of those presented as described in ASTM letter of April 28,.2000.Ball Rust Test instead of Seq. IID; Seq.IVA plus Seq. VG instead of Seq.VE;

Seq.VIII instead of L-38; Seq.IIIF as an alternative to the Seq. IIIE but for this engine test no official document has been released. Current ASTM D4485-01 c does not contain these information yet.

# Table (3-0)

# API " C.." (DIESEL) SERVICE CATEGORIES

ENGINE AND BENCH TEST REQUIREMENT SUMMARY

| CI-4 | CH-4 | CG-4 | CF-4 | (CE) | CF-2 | (CF) | API classification | (CD-II) | (CD) | (CC) | (CB) | (CA) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| all |  | Grade | all |
| current | current | current | current | Obsol. | current | current | Timing | Obsol. | Obsol. | Obsol. | Obsol. | Obsol. |
| - - IIIF 1R+(1K or 1N) - - - - T-8E - X M11 EGR - X | - - IIIE 1P+1K - - - - T-8E X - M11 - X | - X IIIE 1N - - - - T-8 - - - - X | - X - 1K - - orT-9 X X or T-8A - - - - X - | X - - 1G2 - - X X - - - - - - | - X - 1M-PC - X - - - - - - - - | - - - 1M-PC - - - - - - - - - - - | L-38 SEQ. VIII SEQ. III CATERPILLAR DD6V-53T DD6V-92TA MACK T-6 MACK T-7 MACK T-8 / T-8E MACK T-9 MACK T-10 CUMMINS M11/M11 EGR CUMMINS NTC-400 RFWT EOAT Aeration Navistar | X - - 1G2 X - - - - - - - - - -- | X - - 1G2 - - - - - - - - - - | X - - 1H/1H2 - - - - - - - - - - | X - - L1 - - - - - - - - - - | X - - L1 - - - - - - - - - - |
| SAE J300 |  | Visco., HT/HS, pumpab. | SAE J300 |
| X X X X X | X X X - - | X X - - - | - X - - - | - - - - - | - X - - - | - X - - - | Cummins corrosion Metals, AN, BN Volatility Foaming Elastomer compatibility | - - - - | - - - - - | - - - - - | - - - - - | - - - - - |

# Table (3-1)

# API " C.." (DIESEL) SERVICE CATEGORIES

BENCH TEST LIMITS

| CI-4 | CH-4 | CG-4 | CF-4 | CF-2 | CF | API Designation |
| --- | --- | --- | --- | --- | --- | --- |
| all | Viscosity Grades |
| current | Timing |
| 10 / 01 20 / 01 10 / 01 | 10 / 01 20 / 01 10 / 01 | 10 / 01 20 / 01 10 / 01 | - - - | - - - | - - - | ASTM D892 Foaming settling Sequence I, ml max. Sequence II, ml max. Sequence III, ml max. |
| - X 20 120 50 3 | - X 20 120 50 3 | X - 20 60 report 3 | X - 20 60 report 3 | - - - - | - - - - | Cummins Corrosion (HTCBT) ASTM D5968 (CBT @ 121 oC) ASTM D6594(HTCBT @ 135 oC) ppm increase, max. copper Lead Tin Copper corrosion acc. to ASTM D130, max. |
| 3.5 min. | SAE J300 | SAE J300 | SAE J300 | SAE J300 | SAE J300 | ASTM D4683, HT/HS viscosity mPa.s, min. |
| SAE J300 | SAE J300 | SAE J300 | SAE J300 | SAE J300 | SAE J300 | ASTM D445, kinematic viscosity at 100oC cSt, |
| SAE J300 | SAE J300 | SAE J300 | SAE J300 | SAE J300 | SAE J300 | ASTM D5293, low tem. cranking visc. cP at -xx oC |
| SAE J300(2) | SAE J300 | SAE J300 | SAE J300 | SAE J300 | SAE J300 | ASTM D4684, pumpability 60.000 cP max. at oC |
| 10W-30 15W-40 20 18 17 15 | - - | - - | - - | ASTM D5800, volatility % loss at 250 oC, max. Or ASTM D6417, volatility % loss at 371 oC, max. |
| stay in grade | XW-40 12.5 | XW-30 9.3 |  |  |  | ASTM D6278, shearing kin. visc. @100 oC after shearing, cSt, min. |
| pass pass pass pass |  |  |  |  |  | Elastomer Compatibility Nitrile Silicone Polyacrylate FKM |

(1) 10 minutes settling                                                               (2) There is an additional requirement on pumpability performance of  the 75 h. used oil from Mack T-10.

(3-2) Table

# API " C.." (DIESEL) SERVICE CATEGORIES

ENGINE TEST LIMITS-1

| Cl-4 | CH-4 | CG-4 | CF-4 | Letter designation | (CE) | CF-2 | CD-II | CF |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| all | all | all | all | SAE Viscosity grades | all | all | all | all |
| - - - - | - - - - | 4)) 1-2-3 43.7-48.1-50 - 0.5(2) (5 | 4)) - 50 - - | CRC L- 38 Run number Bearing weight loss, mg max. Piston skirt varnish, min. Used oil vis.; cSt > SAE grade limit, min. | - 50 - - | (4) 1-2-3 43.7-48.1-50 - - | - 50 9.0 - | (4) 1-2-3 43.7-48.1-50 - - |
| - | - | (4) 1-2-3 29.3-31.9-33 0.5 (5) | (4) - 33.0 - | SEQUENCE VIII Run number Bearing weight loss, mg max. Used oil vis. cSt > SAE grade limit, min. | - | (4) 1-2-3 29.3-31.9-33 | - | (4) 1-2-3 29.3-31.9-33 |
| IIIF - - 275 5.2 | IIIE - - <200 - | IIIE 1-2-3 67.5-65.1-64 - - | - | SEQUENCE III Run number Hours to 375 % vis. Inc. at 40oC, min. 64h. vis. Inc. from 10mn sample at40oC, % Oil consumption/liter, max. | - | - | - | - |
| 1N(3) 1-2-3 20-23-25 286.2-311.7-323 3-4-5 - none none 0.5 - | 1K 1-2-3 24-27-29 332-347-353 4-5-5 - none - 0.5 - | 1N 1-2-3 20-23-25 286.2-311.7-323 3-4-5 - none none 0.5 - | 1K 1-2-3 24-26-27 332-339-342 4-4-5 - - none 0.5 0.27 | CATERPILLAR Run number Top groove fill, % max. Weighted total demerit, max. Top land heavy carbon (TLHC), % max. Ring side clear. Loss, mm (in) max. Ring and liner scuffing Ring sticking Avg. oil cons., g/kWh max., 0-252h Avg. oil cons., g/kWh max., 240-252h | 1G2 - 80 300 - 0.013 (0.0005) - - - - | 1M-PC - - 100(1) - - - - - - | 1G2 - 80 300 - 0.013 - - - - | 1M-PC - 70 240 - 0.013 none none - - |
| 1R 1-2-3 52-57-59 382-396-402 31-35-36 none none - 13.1 initial + 1.8 - | 1P 1-2-3 36-39-41 350-378-390 40-46-49 none - 12.4 - - 14.6 | - | - | CATERPILLAR Run number Top groove carbon fill, % max. Weighted total demerit, max. Top land carbon (TLC), % max. Ring and liner scuffing Ring sticking Avg. oil cons., g/h max., 0-360h Initial oil cons., g/h max., 0-252h Final oil cons., g/h max., 432-504h Final oil cons., g/h max., 312-360h | - | - | - | - |

# Table (3-3)

# API " C.." (DIESEL) SERVICE CATEGORIES

ENGINE TEST LIMITS-2

| Cl-4 | CH-4 | CG-4 | CF-4 | Letter designation | (CE) | CF-2 | CD-II | CF |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| all | all | all | all | SAE Viscosity grades | all | all | all | all |
| M11 EGR 1-2-3 - 20.0-21.8-22.6 275-320-341 7.8-7.6-7.5 175-186-191 | M11 1-2-3 6.5-7.5-8.0 - 79-93-100 8.7-8.6-8.5 - | - | - | CUMMINS M11/ M11 EGR Run number Rocker pad avg. wt loss norm. to 4.5% soot, µm, max. Crosshead total wt. loss norm. to 4.6% soot, µm, max. Oil filter ∆P at EOT, kPA, max. Engine sludge, CRC merit at EOT, min. Top ring weight loss, mg, max. | - | - | - | - |
| - | - | - | (1) < ref oil 0.002 15 | CUMMINS NTC 400 Oil cons. ( 2nd order regression) Cam follower pin wear, in max. Crown land heavy carbon, % max. | Pass (2) 0.002 15 | - | - | - |
| - | - | - | - | DETROIT DIESEL Run number Weighted total demerit avg., max. Hot stuck rings Average liner scuffing, area %, max. Liner distress, avg. % area, max. Liner distress, avg. % max., 1 cyl Valve distress Face distress, avg.fire ring, dem. Max. Face distr., avg. 2nd + 3rd ring, dem. Max. | - | DD6V92TA 1-2-3 - - 45-48-50 2-2-2 5-5-5 - 0.23-0.24-0.26 0.20-0.21-0.22 | DD6V53T - 400 none - 12.0 - none - 13.0 | - |
| 1-2-3 0.3-0.33-0.36 (7.6-8.4-9.1) | 1-2-3 0.3-0.33-0.36 (7.6-8.4-9.1 | 1-2-3 0.45-0.49-0.5 (11.4-12.4-12.7) | - | ROLLER FOLLOWER WEAR TEST (RWFT) Run number Avg. Pin wear, mils max., Avg. Pin wear, (µm) max. | - | - | - | - |
| 8 | 8 | 10 | - | ENGINE OIL AERATION TEST (EOAT) Oil Aeration at 20 h., % max. | - | - | - | - |

(1) Cummins NTC 400 can be replaced by one additional Cat 1K  meeting CF-4 limit.

(2) Oil consumption must be lower than ref. oil one + 1 std deviation.

# Table (3-4)

# API " C.." (DIESEL) SERVICE CATEGORIES

| Cl-4 | CH-4 | CG-4 | CF-4 | Letter designation | (CE) | CF-2 | CD-II | CF |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| all | all | all | all | SAE Viscosity grades | all | all | all | all |
| - | - | - | (7) 0.0014 200(1) 14 650 0.20 90(2) | Mack T- 6 Oil cons., lb/bhp-hr, max. Avg. 1st+2nd ring wt. loss, mg max. Visc.inc., cSt, max. Piston demerit, max. Maximum ring proudness, in. Merit rating, in. | - - - - - 90 | - | - | - |
| - | - | - | (8) 0.040 | Mack T-7 Avg.rate of vis.inc. at 100oC/h. for last 50h, cSt/h, max | 0.040 | - | - | - |
| T-8E 1-2-3 - 1.8-1.9-2.0(4) - - - | T- 8Eُُ 1-2-3 - 2.1-2.2-2.3(3) 11.5-12.5-13 - - | T- 8 1-2-3 - - 11.5-12.5-13.0 138(20) 0.0005(0.304) | T- 8 (8) 0.20 - - - - | Mack Run number 100-150 hour avg. rate of vis. Inc, at 100oC/h,cSt/h,max Relativity viscosity at 100oC at 4.8% soot, max. Visc. inc.at 100oC at 3.8% soot,cSt max. Filter plugging, diff.press, kPa (psi) max. Oil consumption, avg. lb/bhp-h(g/kWh), max. | - | - | - | - |
| - | 1 - 2 - 3 25.4-26.6-27.1 120-136-144 25-32-36 | - | (7) 40 150 - | Mack T- 9 Avg. liner wear norm. to 1.75% soot, µm max. Average top ring wt. loss, mg max. Pb increase, ppm, max. | - | - | - | - |
| 1000 30 140 30 10 57 25000(NYS) (6) | - | - | - | Mack T-10 Merit rating, min. Liner wear, µm max. Top ring wt. loss, mg, max. EOT lead change ppm, max. 250-300 hour lead change ppm, max. Avg.oil consumption phase 2, g/hr, max. Used oil pumpability at75h, MRV @ -20oC, cP, max.(5) | - | - | - | - |

# ENGINE TEST LIMITS-3

# TABLE (4)

Pour Point and Flash Point of Engine Oils

| Oil Grades | Pour Point ASTM D97 oC (max.) | Flash Point ASTM D92 oC (min.) |
| --- | --- | --- |
| 0 W* | -39 | 185 |
| 5 W | -36 | 195 |
| 10 W | -33 | 205 |
| 15 W | -27 | 210 |
| 20 W | -24 | 215 |
| 25 W | -24 | 220 |
| 20 | -21 | 215 |
| 30 | -18 | 220 |
| 40 | -15 | 230 |
| 50 | -9 | 235 |
| 60 | -9 | 240 |

# * W:  For Winter

# TABLE ( 5)

# API Classification  of Base Oil Groups

| Base Oil Category | Sulfur (%) | Saturates (%) | Viscosity Index |
| --- | --- | --- | --- |
| Group I | >0.03 and/or < 90 | 80 to 120 |
| Group II | ≤0.03 and ≥ 90 | 80 to 120 |
| Group III | ≤ 0.03 and ≥ 90 | ≥ 120 |
| Group IV | All polyalphaolefins (PAOs) |
| Group V | All others not included in Group I,II,III or IV |

# TABLE (6)

Service Classification Engine oils , Engine Test Requirements

& ASTM Methods

| API | Engine Test Requirement | ASTM Test Method |
| --- | --- | --- |
| SJ | CRC L-38 | ASTM D 5119 |
|  | Sequence IID | ASTM D 5844 |
|  | Sequence IIIE | ASTM D 5533 |
|  | Sequence VE | ASTM D 5302 |
| SL | Sequence IIIF | ASTM RR D02-1491 |
|  | Sequence IVA | ASTM RR D02-1473 |
|  | Sequence VG | ASTM D 6593 |
|  | Sequence VIII | ASTM D 6709 |
| SM | Sequence VIII | ASTM D 6709 |
|  | BRT | ASTM D 6557 |
|  | Sequence IVA | ASTM RR D02-1473 |
|  | Sequence VG | ASTM D 6593 |

# TABLE (7)

Commercial  Classification Engine oils , Engine Test Requirements

& ASTM Methods

| API | Engine Test Requirement | ASTM Test Method |
| --- | --- | --- |
| CF | CRC L-38 | ASTM D 5119 |
|  | Caterpillar 1M-PC | ASTM D 6618 |
| CF-2 | CRC L-38 | ASTM D 5119 |
|  | Caterpillar 1M-PC | ASTM D 6618 |
|  | Detroit Diesel 6V92TA | ASTM D 5862 |
| CF-4 | CRC L-38 | ASTM D 5119 |
|  | Mack T-7 | ASTM RR D02-1220 |
|  | Caterpillar 1K | ASTM RR D02-1273 |
| CG-4 | CRC L-38 | ASTM D 5119 |
|  | Sequence IIIE | ASTM D 5533 |
|  | Roller Follower Wear | ASTM D 5966 |
|  | Mack T-8 | ASTM D 5967 |
|  | Caterpillar 1N | ASTM RR D02-132 |
| CH-4 | Sequence IIIE | ASTM D 5533 |
|  | Roller Follower Wear | ASTM D 5966 |
|  | Mack T-8E | ASTM D 5967 |
|  | Mack T-9 | ASTM D6483 |
|  | Cummins M 11 | ASTM RR D02-1439 |
|  | Caterpillar 1P | ASTM D 6681 |
|  | Caterpillar 1K | ASTM RR D02-1273 |
| CI-4 | Caterpillar 1R | ASTM RR D02-BO |
|  | Cummins M 11 | ASTM RR D02-1439 |
|  | Mack T-8E | ASTM D 5967 |
|  | Mack T-10 | ASTM RR D02-BO |
|  | Roller Follower Wear | ASTM D 5966 |
|  | Caterpillar 1K or 1N , Heui | ASTM RRD02 1273/1321 |
|  | Sequence IIIF | ASTM RR D02 1491 |

# REFERENCES

# Main Reference

- Recommended Practices and Information Reports of Society of    Automotive Engineers:

SAE  J  300/2004  Engine Oil Viscosity Classification

-       Standard of American Petroleum Institute ( API ):

# API 1509, Engine Oil Licensing and Certification System 15th Ed,    April 2002, and The Attachment 1 to API 1509 15th Ed.

# Other References

American Society for Testing and  Materials, Special    Technical Issue(ASTM)

-ASTM - STP 509 A Part 1:            (Caterpillar 1 G2)

-ASTM - ATP 509 A Part 2:           (Caterpillar 1 H2 Test Method)

# Text boxes

(1) Rating of top and  2nd groove carbon and land carbon.           (2) To measure at 10,20,30 and 40 hours.    (3)  Oils shall  pass either Cat  1k  or  Cat 1N. Cat 1k limits are those required for API CH-4 plus  no ring sticking.

(4) ASTM D4485-01 a issue shows that a sequence VIII is required  to meet API CF, API CF-2 and API CG-4.                       (5)  Limit do not apply to monograde oils.

(1) 151 mg or greater gives 0 Mack merit.                                                              (2) All individual ratings must be greater than 0.                           (3) New oil vis. Minus 50% of ASTM D3945 vis. loss as denominator

(4) Relative Viscosity =Viscosity at 4.8% soot /.Viscosity of new oil sheared in ASTM D6278.

(5) Sample to test can also be from a T-10A test (proposed name given to T-10 test run for 75h to generate the sample for ASTM D4684 as used to measure this parameter.

(6) If yield stress is detected, use modified ASTM D4684,(external preheat); then limits become viscosity: 25.000 cP max and yield stress, <35 Pa.

(7) A Mack T-9 test and its limits (as reported in CF-4 above) can be used as an alternate for the Mack T-6 test.

(8) A Mack T-8A test version and its limits (as reported in CF-4 above) can be used as an alternate for  the Mack T-7 test.